Table 1. Tensile strength and percentage elongation for the leather fatliquored without the addition of oregano oil

| Specimen No. and its orientation to the backbone | Thickness mm | Breaking force N | Tensile strength MPa | Elongation % |
| --- | --- | --- | --- | --- |
|  | parallel |  |  |  |
| 1 | 1.83 | 254.72 | 13.92 | 55.00 |
| 2 | 1.67 | 252.65 | 15.13 | 57.34 |
| 3 | 1.54 | 208.45 | 13.54 | 58.00 |
| 4 | 1.56 | 212.02 | 13.59 | 52.00 |
| 5 | 1.61 | 216.08 | 13.42 | 47.34 |
| 6 | 1.67 | 221.80 | 13.28 | 51.66 |
| 7 | 1.65 | 219.82 | 13.32 | 55.66 |
| 8 | 1.65 | 219.20 | 13.28 | 53.34 |
| 9 | 1.59 | 215.48 | 13.55 | 53.34 |
| a/ | 1.64 | 224 | 13.7 | 53 |
| sdb/ | 0.09 | 17 | 0.6 | 3.3 |
|  | perpendicularly |  |  |  |
| 1 | 1.53 | 157.38 | 10.29 | 64.66 |
| 2 | 1.57 | 169.96 | 10.83 | 65.00 |
| 3 | 1.56 | 162.14 | 10.39 | 64.66 |
| 4 | 1.59 | 171.38 | 10.78 | 61.00 |
| 5 | 1.63 | 172.18 | 10.56 | 76.34 |
| 6 | 1.67 | 178.85 | 10.71 | 71.66 |
| 7 | 1.79 | 210.04 | 11.73 | 66.66 |
| 8 | 1.74 | 195.02 | 11.21 | 68.66 |
| 9 | 1.72 | 179.83 | 10.46 | 69.34 |
| a/ | 1.64 | 177 | 10.8 | 67 |
| sdb/ | 0.09 | 16 | 0.5 | 4.6 |
| a/ arithmetic mean, b/ standard deviation. |  |  |  |  |

Source: own research.

Table 2. Tensile strength and percentage elongation for the leather fatliquored with the addition of oregano oil

| Specimen No. and its orientation to the backbone | Thickness mm | Breaking force N | Tensile strength MPa | Elongation % |
| --- | --- | --- | --- | --- |
|  | parallel |  |  |  |
| 1 | 1.77 | 325.54 | 18.39 | 52.00 |
| 2 | 1.69 | 277.77 | 16.44 | 50.34 |
| 3 | 1.60 | 235.41 | 14.71 | 52.34 |
| 4 | 1.65 | 271.01 | 16.42 | 50.66 |
| 5 | 1.61 | 250.99 | 15.59 | 46.34 |
| 6 | 1.63 | 270.16 | 16.57 | 56.00 |
| 7 | 1.71 | 289.46 | 16.93 | 45.66 |
| 8 | 1.61 | 262.41 | 16.30 | 41.00 |
| 9 | 1.71 | 307.59 | 17.99 | 52.34 |
| a/ | 1.66 | 276 | 16.6 | 50 |
| sdb/ | 0.06 | 27.7 | 1.1 | 4.5 |
|  | perpendicularly |  |  |  |
| 1 | 1.69 | 224.73 | 13.30 | 72.00 |
| 2 | 1.67 | 224.39 | 13.44 | 62.34 |
| 3 | 1.56 | 158.54 | 10.16 | 60.00 |
| 4 | 1.59 | 174.26 | 10.96 | 63.00 |
| 5 | 1.67 | 186.83 | 11.19 | 71.34 |
| 6 | 1.57 | 170.63 | 10.87 | 63.34 |
| 7 | 1.56 | 168.54 | 10.80 | 66.00 |
| 8 | 1.62 | 174.83 | 10.79 | 66.66 |
| 9 | 1.75 | 252.68 | 14.44 | 69.34 |
| a/ | 1.63 | 192 | 11.8 | 66 |
| sdb/ | 0.07 | 32.7 | 1.5 | 4.2 |
| a/ arithmetic mean, b/ standard deviation. |  |  |  |  |

Source: own research.

Table 3. Comparison of tensile strength and percentage elongation for individual kinds of leathers

| Leather | Tensile strength |  | Elongation |  |
| --- | --- | --- | --- | --- |
|  | a/ MPa | sdb/ | a/ % | sdb/ |
| fatliquored without oregano oil | 12.2 | 1.6 | 61 | 8.1 |
| fatliquored with the addition of oregano oil (3%) | 14.2 | 2.8 | 58 | 9.4 |
| a/ arithmetic mean, b/ standard deviation. |  |  |  |  |

Source: own research.

Table 4. Tear load for the leather fatliquored without the addition of oregano oil

| Specimen No. and its orientation to the backbone | Thickness mm | Tear load N | Thickness mm | Tear load N |
| --- | --- | --- | --- | --- |
|  | parallel |  | perpendicularly |  |
| 1 | 1.85 | 41.88 | 1.63 | 38.02 |
| 2 | 1.56 | 38.37 | 1.54 | 28.77 |
| 3 | 1.62 | 39.29 | 1.60 | 34.53 |
| a/ | 1.68 | 40 | 1.59 | 34 |
| sdb/ | 0.15 | 1.8 | 0.05 | 4.7 |
| a/ arithmetic mean, b/ standard deviation. |  |  |  |  |

Source: own research.

Table 5. Tear load for the leather fatliquored with the addition of oregano oil (3%)

| Specimen No. and its orientation to the backbone | Thickness mm | Tear load N | Thickness mm | Tear load N |
| --- | --- | --- | --- | --- |
|  | parallel |  | perpendicularly |  |
| 1 | 1.67 | 43.37 | 1.60 | 27.53 |
| 2 | 1.69 | 57.06 | 1.61 | 31.36 |
| 3 | 1.58 | 30.15 | 1.53 | 23.56 |
| a/ | 1.65 | 44 | 1.58 | 27 |
| sdb/ | 0.06 | 13.5 | 0.04 | 3.9 |
| a/ arithmetic mean, b/ standard deviation. |  |  |  |  |

Source: own research.

Table 6. Comparison of tear load for individual kinds of leather

| Leather | Tear load |  |
| --- | --- | --- |
|  | a/ N | sdb/ |
| fatliquored without oregano oil | 37 | 4.6 |
| fatliquored with the addition of oregano oil (3%) | 36 | 12.5 |
| a/ arithmetic mean, b/ standard deviation. |  |  |

Source: own research.

Table 7. The results of testing the hypothesis on normal distribution of test results

| Leather | Tensile strength |  | Elongation |  | Tear load |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 2 | p | 2 | p | 2 | p |
| fatliquored without oregano oil | 11.25 | 0.277 | 3.59 | 0.999 | 1.67 | 0.989 |
| fatliquored with the addition of oregano oil (3%) | 10.52 | 0.310 | 3.87 | 0.998 | 7.49 | 0.824 |

Source: own research.

Table 8. Results of testing the hypothesis on homogeneity of variation

| Leather | Tensile strength | Elongation | Tear load |
| --- | --- | --- | --- |
|  | s2d |  |  |
| fatliquored without oregano oil | 2.48 | 65.23 | 21.12 |
| fatliquored with the addition of oregano oil (3%) | 7.83 | 88.89 | 75.72 |
|  | Calculated values of Fmax |  |  |
|  | 3.15 | 1.36 | 3.58 |
|  | Limit value Fmax (α = 0.05) = 5.93 |  |  |

Source: own research.

Table 9. Differentiation of tensile strength, percentage elongation and tear load depending on the kind of leather - results of analysis of variance

| Leather | Tensile strength MPa | Elongation % | Tear load N |
| --- | --- | --- | --- |
| fatliquored without oregano oil | 12.22 | 60.65 | 36.81 |
| fatliquored with the addition of oregano oil (3%) | 14.18 | 57.82 | 35.51 |
|  | Analysis of variance |  |  |
| F | 6.71 | 0.94 | 0.05 |
| p | 0.014 | 0.340 | 0.815 |

Source: own research.